# Text boxes

METHOD:

1.  Start with a flat surface. Pick over any rocks

and rake the dirt until it is smooth. We removed the old mulch and added it to the garden beds as it had begun to compost down quite nicely.

2.  Cover the surface with Geotech fabric taking care to make sure that it will not be visible along the edges of the garden.

3.  In the wheelbarrow add gravel and cement.

For a flat area, add 10 parts of gravel to 1 part cement. For any sort of slope, add 5 parts of gravel to 1 part cement.

Mix well (do not add water).

4.  Place the gravel/cement dry mix where the path is to be. We did a layer of approximately 5cm depth to begin with. Repeat this until the area that you are doing is completely covered. You can do any length at one go, but it needs to be completed to the rolled stage before it can be left.

5.  Rake well to ensure as smooth a surface as possible.

6.  Spray the entire gravelled surface with the hose until well-soaked.

7.  Roll the entire area taking care to start at one end and finish at the other so as not to disturb  what you have already completed.

8.  Use the block of wood and the mallet to tamp down any edges that the roller can’t get to.

9.  Repeat the process so that you have approximately 10 cm cover. This can be done at a later stage, or immediately after the first layer.

We are thrilled with the look and the wear of our paths so a huge thanks to June and Bill for sharing their expertise (among other things).

Celeste and Peter Shadie